## Slide 1: 160311
TEST AFTER NORMALIZE THE DATA

## Slide 2: Normalization
Import refData and testData
Both in Time Domain
Transfer refData and testData  Frequency Domain
Same function
Same length
Normalization:
x_fft = x_fft/x_fftR
x_power = x_power/x_powerR

## Slide 3: Power after normalize
Test Data
Data after Normalize

## Slide 4: Power after normalize
Test Data
Data after Normalize
Ref Data

## Slide 5: Test Result
Still, I used both solvers to test 41 different frequencies (from ~0.7THz to 1THz) with 5 different thickness (from 10 μm to 30 μm in an interval of 5μm)
· Very thick model(only order 1 is considered, that is, no further reflection inside the material afer the first reflection)
Chart: Real Part of n2
10μm | 2.7646 | 2.7516 | 2.7387 | 2.7261 | 2.7136 | 2.7014 | 2.6893 | 2.6774 | 2.6657 | 2.6542 | 2.6428 | 2.6317 | 2.6206 | 2.6098 | 2.5991 | 2.5886 | 2.5781 | 2.5679 | 2.5578 | 2.5478 | 2.538 | 2.5282 | 2.5186 | 2.5092 | 2.4999 | 2.4907 | 2.4816 | 2.4726 | 2.4637 | 2.455 | 2.4464 | 2.4378 | 2.4294 | 2.4211 | 2.4128 | 2.4047 | 2.3966 | 2.3887 | 2.3809 | 2.3731 | 2.3655
15μm | 2.3284 | 2.3177 | 2.3071 | 2.2967 | 2.2865 | 2.2765 | 2.2666 | 2.2569 | 2.2472 | 2.2378 | 2.2285 | 2.2192 | 2.2102 | 2.2013 | 2.1925 | 2.1838 | 2.1753 | 2.1669 | 2.1586 | 2.1504 | 2.1423 | 2.1343 | 2.1264 | 2.1187 | 2.111 | 2.1034 | 2.096 | 2.0886 | 2.0813 | 2.0742 | 2.0671 | 2.0601 | 2.0532 | 2.0462 | 2.0395 | 2.0329 | 2.0262 | 2.0197 | 2.0132 | 2.0069 | 2.0006
20μm | 2.0671 | 2.0577 | 2.0486 | 2.0395 | 2.0307 | 2.0219 | 2.0132 | 2.0048 | 1.9964 | 1.9882 | 1.9801 | 1.9721 | 1.9643 | 1.9564 | 1.9489 | 1.9413 | 1.9338 | 1.9266 | 1.9192 | 1.9121 | 1.9051 | 1.8982 | 1.8914 | 1.8846 | 1.8779 | 1.8713 | 1.8648 | 1.8584 | 1.8521 | 1.8458 | 1.8396 | 1.8335 | 1.8275 | 1.8216 | 1.8156 | 1.8098 | 1.804 | 1.7984 | 1.7928 | 1.7872 | 1.7818
25μm | 1.8879 | 1.8796 | 1.8714 | 1.8632 | 1.8553 | 1.8474 | 1.8396 | 1.8319 | 1.8245 | 1.8171 | 1.8098 | 1.8027 | 1.7955 | 1.7886 | 1.7818 | 1.775 | 1.7682 | 1.7616 | 1.7552 | 1.7488 | 1.7424 | 1.7361 | 1.73 | 1.7239 | 1.718 | 1.7119 | 1.7062 | 1.7003 | 1.6947 | 1.689 | 1.6835 | 1.6779 | 1.6725 | 1.6673 | 1.6619 | 1.6566 | 1.6515 | 1.6465 | 1.6412 | 1.6364 | 1.6314
30μm | 1.7552 | 1.7475 | 1.7399 | 1.7324 | 1.7252 | 1.718 | 1.7108 | 1.7038 | 1.6969 | 1.6903 | 1.6835 | 1.6769 | 1.6703 | 1.664 | 1.6577 | 1.6515 | 1.6453 | 1.6393 | 1.6333 | 1.6274 | 1.6216 | 1.6159 | 1.6103 | 1.6047 | 1.5991 | 1.5937 | 1.5883 | 1.583 | 1.5778 | 1.5726 | 1.5676 | 1.5624 | 1.5574 | 1.5526 | 1.5475 | 1.5428 | 1.5382 | 1.5334 | 1.5286 | 1.524 | 1.5194
Chart: Imaginary part of n2
10μm | 2.3351 | 2.3221 | 2.3093 | 2.2966 | 2.2842 | 2.272 | 2.2599 | 2.2481 | 2.2364 | 2.2249 | 2.2135 | 2.2024 | 2.1914 | 2.1805 | 2.1699 | 2.1593 | 2.1488 | 2.1386 | 2.1285 | 2.1185 | 2.1086 | 2.0989 | 2.0893 | 2.0799 | 2.0705 | 2.0613 | 2.0521 | 2.0431 | 2.0342 | 2.0255 | 2.0169 | 2.0082 | 1.9998 | 1.9914 | 1.9831 | 1.975 | 1.9669 | 1.9589 | 1.951 | 1.9432 | 1.9355
15μm | 1.8982 | 1.8874 | 1.8767 | 1.8663 | 1.8559 | 1.8458 | 1.8358 | 1.826 | 1.8162 | 1.8067 | 1.7973 | 1.7879 | 1.7788 | 1.7697 | 1.7608 | 1.752 | 1.7434 | 1.7348 | 1.7264 | 1.7181 | 1.7098 | 1.7017 | 1.6937 | 1.6858 | 1.678 | 1.6703 | 1.6627 | 1.6552 | 1.6478 | 1.6404 | 1.6332 | 1.626 | 1.619 | 1.6119 | 1.605 | 1.5982 | 1.5914 | 1.5847 | 1.5781 | 1.5716 | 1.5651
20μm | 1.6332 | 1.6237 | 1.6143 | 1.605 | 1.5959 | 1.587 | 1.5781 | 1.5694 | 1.5608 | 1.5524 | 1.544 | 1.5358 | 1.5277 | 1.5197 | 1.5119 | 1.5041 | 1.4964 | 1.4889 | 1.4813 | 1.4739 | 1.4667 | 1.4595 | 1.4524 | 1.4454 | 1.4385 | 1.4316 | 1.4248 | 1.4182 | 1.4116 | 1.4051 | 1.3987 | 1.3922 | 1.386 | 1.3798 | 1.3736 | 1.3675 | 1.3614 | 1.3556 | 1.3496 | 1.3438 | 1.3381
25μm | 1.4489 | 1.4402 | 1.4317 | 1.4232 | 1.4149 | 1.4067 | 1.3987 | 1.3906 | 1.3829 | 1.3752 | 1.3675 | 1.36 | 1.3525 | 1.3453 | 1.3381 | 1.331 | 1.3239 | 1.317 | 1.3101 | 1.3034 | 1.2966 | 1.29 | 1.2836 | 1.2771 | 1.2708 | 1.2645 | 1.2583 | 1.2522 | 1.2461 | 1.2401 | 1.2342 | 1.2283 | 1.2225 | 1.2169 | 1.2112 | 1.2055 | 1.2001 | 1.1947 | 1.1891 | 1.1839 | 1.1785
30μm | 1.3101 | 1.302 | 1.294 | 1.2862 | 1.2785 | 1.2708 | 1.2633 | 1.2558 | 1.2485 | 1.2414 | 1.2343 | 1.2272 | 1.2202 | 1.2134 | 1.2067 | 1.2001 | 1.1934 | 1.187 | 1.1806 | 1.1743 | 1.168 | 1.1618 | 1.1558 | 1.1498 | 1.1437 | 1.1379 | 1.1321 | 1.1263 | 1.1207 | 1.1151 | 1.1096 | 1.104 | 1.0985 | 1.0932 | 1.0878 | 1.0826 | 1.0775 | 1.0723 | 1.0671 | 1.0621 | 1.0571
Notes: Test1.xlsx

## Slide 6: Test Result (Normalize vs Non-Normal)
· Very thick model(only order 1 is considered, that is, no further reflection inside the material afer the first reflection)
· Quite close in both value and shape
Chart: Real part of n2
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26 | 27 | 28 | 29 | 30 | 31 | 32 | 33 | 34
10μm | 2.3274 | 2.3176 | 2.3078 | 2.2836 | 2.2744 | 2.2657 | 2.2568 | 2.2482 | 2.2256 | 2.2175 | 2.2094 | 2.2014 | 2.1935 | 2.1724 | 2.1649 | 2.1575 | 2.1505 | 2.1433 | 2.1238 | 2.1169 | 2.1101 | 2.1035 | 2.0969 | 2.0784 | 2.0722 | 2.066 | 2.0599 | 2.054 | 2.0366 | 2.0308 | 2.0251 | 2.0198 | 2.0143 | 1.9975
15μm | 2.0661 | 2.0578 | 2.0497 | 2.0279 | 2.0199 | 2.0123 | 2.0051 | 1.9975 | 1.9772 | 1.9703 | 1.9634 | 1.9566 | 1.95 | 1.9309 | 1.9245 | 1.9183 | 1.9122 | 1.9062 | 1.8884 | 1.8827 | 1.877 | 1.8713 | 1.8659 | 1.8491 | 1.8438 | 1.8386 | 1.8335 | 1.8286 | 1.8125 | 1.8079 | 1.8029 | 1.7983 | 1.7939 | 1.7786
20μm | 1.8872 | 1.8796 | 1.8726 | 1.8523 | 1.8453 | 1.8388 | 1.8322 | 1.8258 | 1.8069 | 1.8009 | 1.7949 | 1.7888 | 1.7829 | 1.7652 | 1.7597 | 1.7542 | 1.7488 | 1.7436 | 1.727 | 1.7221 | 1.7169 | 1.712 | 1.7073 | 1.6916 | 1.6871 | 1.6824 | 1.6779 | 1.6737 | 1.6586 | 1.6545 | 1.6504 | 1.6464 | 1.6424 | 1.628
25μm | 1.7545 | 1.748 | 1.7411 | 1.7221 | 1.716 | 1.7103 | 1.7041 | 1.6983 | 1.6805 | 1.6751 | 1.6695 | 1.6642 | 1.6589 | 1.6424 | 1.6372 | 1.6324 | 1.6278 | 1.623 | 1.6072 | 1.6027 | 1.5982 | 1.5939 | 1.5897 | 1.5745 | 1.5703 | 1.5663 | 1.5624 | 1.5586 | 1.5442 | 1.5405 | 1.5369 | 1.5334 | 1.5298 | 1.516
Chart: Real Part of n2
10μm | 2.7646 | 2.7516 | 2.7387 | 2.7261 | 2.7136 | 2.7014 | 2.6893 | 2.6774 | 2.6657 | 2.6542 | 2.6428 | 2.6317 | 2.6206 | 2.6098 | 2.5991 | 2.5886 | 2.5781 | 2.5679 | 2.5578 | 2.5478 | 2.538 | 2.5282 | 2.5186 | 2.5092 | 2.4999 | 2.4907 | 2.4816 | 2.4726 | 2.4637 | 2.455 | 2.4464 | 2.4378 | 2.4294 | 2.4211 | 2.4128 | 2.4047 | 2.3966 | 2.3887 | 2.3809 | 2.3731 | 2.3655
15μm | 2.3284 | 2.3177 | 2.3071 | 2.2967 | 2.2865 | 2.2765 | 2.2666 | 2.2569 | 2.2472 | 2.2378 | 2.2285 | 2.2192 | 2.2102 | 2.2013 | 2.1925 | 2.1838 | 2.1753 | 2.1669 | 2.1586 | 2.1504 | 2.1423 | 2.1343 | 2.1264 | 2.1187 | 2.111 | 2.1034 | 2.096 | 2.0886 | 2.0813 | 2.0742 | 2.0671 | 2.0601 | 2.0532 | 2.0462 | 2.0395 | 2.0329 | 2.0262 | 2.0197 | 2.0132 | 2.0069 | 2.0006
20μm | 2.0671 | 2.0577 | 2.0486 | 2.0395 | 2.0307 | 2.0219 | 2.0132 | 2.0048 | 1.9964 | 1.9882 | 1.9801 | 1.9721 | 1.9643 | 1.9564 | 1.9489 | 1.9413 | 1.9338 | 1.9266 | 1.9192 | 1.9121 | 1.9051 | 1.8982 | 1.8914 | 1.8846 | 1.8779 | 1.8713 | 1.8648 | 1.8584 | 1.8521 | 1.8458 | 1.8396 | 1.8335 | 1.8275 | 1.8216 | 1.8156 | 1.8098 | 1.804 | 1.7984 | 1.7928 | 1.7872 | 1.7818
25μm | 1.8879 | 1.8796 | 1.8714 | 1.8632 | 1.8553 | 1.8474 | 1.8396 | 1.8319 | 1.8245 | 1.8171 | 1.8098 | 1.8027 | 1.7955 | 1.7886 | 1.7818 | 1.775 | 1.7682 | 1.7616 | 1.7552 | 1.7488 | 1.7424 | 1.7361 | 1.73 | 1.7239 | 1.718 | 1.7119 | 1.7062 | 1.7003 | 1.6947 | 1.689 | 1.6835 | 1.6779 | 1.6725 | 1.6673 | 1.6619 | 1.6566 | 1.6515 | 1.6465 | 1.6412 | 1.6364 | 1.6314
30μm | 1.7552 | 1.7475 | 1.7399 | 1.7324 | 1.7252 | 1.718 | 1.7108 | 1.7038 | 1.6969 | 1.6903 | 1.6835 | 1.6769 | 1.6703 | 1.664 | 1.6577 | 1.6515 | 1.6453 | 1.6393 | 1.6333 | 1.6274 | 1.6216 | 1.6159 | 1.6103 | 1.6047 | 1.5991 | 1.5937 | 1.5883 | 1.583 | 1.5778 | 1.5726 | 1.5676 | 1.5624 | 1.5574 | 1.5526 | 1.5475 | 1.5428 | 1.5382 | 1.5334 | 1.5286 | 1.524 | 1.5194
Normalized
Non-Normalized
Notes: Test1.xlsx

## Slide 7: Test Result (Normalize vs Non-Normal)
· Very thick model(only order 1 is considered, that is, no further reflection inside the material afer the first reflection)
· Quite close in both value and shape
Chart: Imaginary part of n2
10μm | 2.3351 | 2.3221 | 2.3093 | 2.2966 | 2.2842 | 2.272 | 2.2599 | 2.2481 | 2.2364 | 2.2249 | 2.2135 | 2.2024 | 2.1914 | 2.1805 | 2.1699 | 2.1593 | 2.1488 | 2.1386 | 2.1285 | 2.1185 | 2.1086 | 2.0989 | 2.0893 | 2.0799 | 2.0705 | 2.0613 | 2.0521 | 2.0431 | 2.0342 | 2.0255 | 2.0169 | 2.0082 | 1.9998 | 1.9914 | 1.9831 | 1.975 | 1.9669 | 1.9589 | 1.951 | 1.9432 | 1.9355
15μm | 1.8982 | 1.8874 | 1.8767 | 1.8663 | 1.8559 | 1.8458 | 1.8358 | 1.826 | 1.8162 | 1.8067 | 1.7973 | 1.7879 | 1.7788 | 1.7697 | 1.7608 | 1.752 | 1.7434 | 1.7348 | 1.7264 | 1.7181 | 1.7098 | 1.7017 | 1.6937 | 1.6858 | 1.678 | 1.6703 | 1.6627 | 1.6552 | 1.6478 | 1.6404 | 1.6332 | 1.626 | 1.619 | 1.6119 | 1.605 | 1.5982 | 1.5914 | 1.5847 | 1.5781 | 1.5716 | 1.5651
20μm | 1.6332 | 1.6237 | 1.6143 | 1.605 | 1.5959 | 1.587 | 1.5781 | 1.5694 | 1.5608 | 1.5524 | 1.544 | 1.5358 | 1.5277 | 1.5197 | 1.5119 | 1.5041 | 1.4964 | 1.4889 | 1.4813 | 1.4739 | 1.4667 | 1.4595 | 1.4524 | 1.4454 | 1.4385 | 1.4316 | 1.4248 | 1.4182 | 1.4116 | 1.4051 | 1.3987 | 1.3922 | 1.386 | 1.3798 | 1.3736 | 1.3675 | 1.3614 | 1.3556 | 1.3496 | 1.3438 | 1.3381
25μm | 1.4489 | 1.4402 | 1.4317 | 1.4232 | 1.4149 | 1.4067 | 1.3987 | 1.3906 | 1.3829 | 1.3752 | 1.3675 | 1.36 | 1.3525 | 1.3453 | 1.3381 | 1.331 | 1.3239 | 1.317 | 1.3101 | 1.3034 | 1.2966 | 1.29 | 1.2836 | 1.2771 | 1.2708 | 1.2645 | 1.2583 | 1.2522 | 1.2461 | 1.2401 | 1.2342 | 1.2283 | 1.2225 | 1.2169 | 1.2112 | 1.2055 | 1.2001 | 1.1947 | 1.1891 | 1.1839 | 1.1785
30μm | 1.3101 | 1.302 | 1.294 | 1.2862 | 1.2785 | 1.2708 | 1.2633 | 1.2558 | 1.2485 | 1.2414 | 1.2343 | 1.2272 | 1.2202 | 1.2134 | 1.2067 | 1.2001 | 1.1934 | 1.187 | 1.1806 | 1.1743 | 1.168 | 1.1618 | 1.1558 | 1.1498 | 1.1437 | 1.1379 | 1.1321 | 1.1263 | 1.1207 | 1.1151 | 1.1096 | 1.104 | 1.0985 | 1.0932 | 1.0878 | 1.0826 | 1.0775 | 1.0723 | 1.0671 | 1.0621 | 1.0571
Chart: Imaginary part of n2
10μm | 2.3351 | 2.3221 | 2.3093 | 2.2966 | 2.2842 | 2.272 | 2.2599 | 2.2481 | 2.2364 | 2.2249 | 2.2135 | 2.2024 | 2.1914 | 2.1805 | 2.1699 | 2.1593 | 2.1488 | 2.1386 | 2.1285 | 2.1185 | 2.1086 | 2.0989 | 2.0893 | 2.0799 | 2.0705 | 2.0613 | 2.0521 | 2.0431 | 2.0342 | 2.0255 | 2.0169 | 2.0082 | 1.9998 | 1.9914
15μm | 1.8982 | 1.8874 | 1.8767 | 1.8663 | 1.8559 | 1.8458 | 1.8358 | 1.826 | 1.8162 | 1.8067 | 1.7973 | 1.7879 | 1.7788 | 1.7697 | 1.7608 | 1.752 | 1.7434 | 1.7348 | 1.7264 | 1.7181 | 1.7098 | 1.7017 | 1.6937 | 1.6858 | 1.678 | 1.6703 | 1.6627 | 1.6552 | 1.6478 | 1.6404 | 1.6332 | 1.626 | 1.619 | 1.6119
20μm | 1.6332 | 1.6237 | 1.6143 | 1.605 | 1.5959 | 1.587 | 1.5781 | 1.5694 | 1.5608 | 1.5524 | 1.544 | 1.5358 | 1.5277 | 1.5197 | 1.5119 | 1.5041 | 1.4964 | 1.4889 | 1.4813 | 1.4739 | 1.4667 | 1.4595 | 1.4524 | 1.4454 | 1.4385 | 1.4316 | 1.4248 | 1.4182 | 1.4116 | 1.4051 | 1.3987 | 1.3922 | 1.386 | 1.3798
25μm | 1.4489 | 1.4402 | 1.4317 | 1.4232 | 1.4149 | 1.4067 | 1.3987 | 1.3906 | 1.3829 | 1.3752 | 1.3675 | 1.36 | 1.3525 | 1.3453 | 1.3381 | 1.331 | 1.3239 | 1.317 | 1.3101 | 1.3034 | 1.2966 | 1.29 | 1.2836 | 1.2771 | 1.2708 | 1.2645 | 1.2583 | 1.2522 | 1.2461 | 1.2401 | 1.2342 | 1.2283 | 1.2225 | 1.2169
Normalized
Non-Normalized
Notes: Test1.xlsx

## Slide 8: Test Result
· Order 2
Chart: Real Part of n2
10μm | 0.76499 | 0.76706 | 0.76545 | 0.76735 | 0.76962 | 0.77163 | 0.76969 | 0.77192 | 0.77392 | 0.77599 | 0.77409 | 0.77617 | 0.77806 | 0.77606 | 0.77816 | 0.78016 | 0.78222 | 0.77989 | 0.78173 | 0.78371 | 0.78178 | 0.78366 | 0.78567 | 0.78756 | 0.78531 | 0.78725 | 0.78904 | 0.79102 | 0.78861 | 0.79048 | 0.79231 | 0.79004 | 0.7918 | 0.7937 | 0.79539 | 0.79302 | 0.79467 | 0.7965 | 0.79815 | 0.79562 | 0.79716
15μm | 0.80172 | 0.80011 | 0.80243 | 0.80455 | 0.80287 | 0.80562 | 0.80805 | 0.80594 | 0.80839 | 0.80649 | 0.80846 | 0.81076 | 0.80872 | 0.81069 | 0.81301 | 0.81097 | 0.81312 | 0.81536 | 0.81321 | 0.81569 | 0.8178 | 0.81533 | 0.81764 | 0.81978 | 0.81687 | 0.81928 | 0.82076 | 0.81855 | 0.82102 | 0.82272 | 0.81993 | 0.82147 | 0.82394 | 0.82142 | 0.82292 | 0.82463 | 0.82261 | 0.824 | 0.82599 | 0.82738 | 0.82478
20μm | 0.81993 | 0.82288 | 0.82562 | 0.82292 | 0.8254 | 0.82323 | 0.82595 | 0.82791 | 0.82527 | 0.82795 | 0.82591 | 0.82833 | 0.82985 | 0.82747 | 0.82867 | 0.83094 | 0.82897 | 0.82944 | 0.83239 | 0.83287 | 0.83081 | 0.83377 | 0.83418 | 0.8321 | 0.83251 | 0.83293 | 0.83585 | 0.83877 | 0.83405 | 0.83698 | 0.83734 | 0.83513 | 0.84064 | 0.83838 | 0.83875 | 0.84164 | 0.83677 | 0.83966 | 0.83998 | 0.83765 | 0.83796
25μm | 0.83443 | 0.8324 | 0.83293 | 0.83595 | 0.83388 | 0.83689 | 0.83734 | 0.83522 | 0.83822 | 0.83864 | 0.84164 | 0.83684 | 0.83982 | 0.84021 | 0.83796 | 0.84094 | 0.84129 | 0.83897 | 0.8446 | 0.84227 | 0.84522 | 0.84554 | 0.84312 | 0.84071 | 0.84639 | 0.84397 | 0.84424 | 0.84174 | 0.84201 | 0.84495 | 0.8452 | 0.84266 | 0.84561 | 0.8458 | 0.84326 | 0.84899 | 0.84641 | 0.84661 | 0.84395 | 0.84694 | 0.84708
30μm | 0.8446 | 0.84232 | 0.83998 | 0.84301 | 0.84066 | 0.84639 | 0.84403 | 0.8416 | 0.84192 | 0.84492 | 0.84519 | 0.84271 | 0.8457 | 0.84316 | 0.84341 | 0.84641 | 0.84384 | 0.84403 | 0.84699 | 0.84722 | 0.84461 | 0.84758 | 0.84777 | 0.85071 | 0.84521 | 0.84819 | 0.84547 | 0.84558 | 0.84852 | 0.84576 | 0.84587 | 0.84877 | 0.84885 | 0.85184 | 0.85188 | 0.84901 | 0.84619 | 0.852 | 0.84621 | 0.84915 | 0.84619
Chart: Imaginary part of n2
10μm | 0.96508 | 0.96336 | 0.95706 | 0.95516 | 0.95375 | 0.95201 | 0.94544 | 0.94401 | 0.94232 | 0.94072 | 0.93434 | 0.93279 | 0.93101 | 0.92462 | 0.92314 | 0.92155 | 0.92004 | 0.91339 | 0.91166 | 0.91009 | 0.90402 | 0.90237 | 0.90089 | 0.89926 | 0.89295 | 0.89142 | 0.88972 | 0.88827 | 0.88189 | 0.88033 | 0.87872 | 0.87262 | 0.87097 | 0.86949 | 0.86778 | 0.86167 | 0.85994 | 0.85843 | 0.85673 | 0.85056 | 0.84877
15μm | 0.83664 | 0.82998 | 0.82743 | 0.82467 | 0.81808 | 0.81603 | 0.81366 | 0.80675 | 0.80446 | 0.79787 | 0.79514 | 0.79275 | 0.78615 | 0.78348 | 0.78117 | 0.7747 | 0.77225 | 0.76992 | 0.76347 | 0.76139 | 0.75897 | 0.75233 | 0.75015 | 0.74781 | 0.74089 | 0.73885 | 0.73596 | 0.7298 | 0.72784 | 0.72519 | 0.71864 | 0.7159 | 0.71398 | 0.70777 | 0.70505 | 0.70252 | 0.69684 | 0.69407 | 0.69183 | 0.68907 | 0.68304
20μm | 0.71864 | 0.71577 | 0.71274 | 0.70505 | 0.70184 | 0.69474 | 0.69179 | 0.68822 | 0.68087 | 0.67795 | 0.67121 | 0.66813 | 0.66432 | 0.65745 | 0.65346 | 0.65034 | 0.64393 | 0.63945 | 0.63692 | 0.63249 | 0.62619 | 0.62371 | 0.61932 | 0.61313 | 0.6088 | 0.60451 | 0.60206 | 0.59961 | 0.59172 | 0.58932 | 0.58509 | 0.57914 | 0.57852 | 0.57259 | 0.56847 | 0.5661 | 0.55851 | 0.55617 | 0.55211 | 0.54637 | 0.54235
25μm | 0.61715 | 0.60987 | 0.60451 | 0.60099 | 0.59385 | 0.59037 | 0.58509 | 0.5781 | 0.57467 | 0.56948 | 0.5661 | 0.55749 | 0.55413 | 0.54907 | 0.54235 | 0.53906 | 0.53407 | 0.52746 | 0.52584 | 0.5193 | 0.51606 | 0.5112 | 0.50476 | 0.49837 | 0.49678 | 0.49047 | 0.48575 | 0.4795 | 0.47486 | 0.47175 | 0.46713 | 0.46104 | 0.45797 | 0.45341 | 0.44744 | 0.44586 | 0.43994 | 0.43549 | 0.42963 | 0.42667 | 0.42226
30μm | 0.52584 | 0.51832 | 0.51085 | 0.50669 | 0.49933 | 0.49678 | 0.48953 | 0.48232 | 0.47672 | 0.47269 | 0.46713 | 0.46012 | 0.45615 | 0.44923 | 0.44384 | 0.43994 | 0.43317 | 0.42787 | 0.42401 | 0.41878 | 0.41222 | 0.40842 | 0.40329 | 0.39949 | 0.39178 | 0.38806 | 0.38177 | 0.37681 | 0.37314 | 0.36699 | 0.36213 | 0.3585 | 0.35368 | 0.35011 | 0.34534 | 0.33945 | 0.33365 | 0.33127 | 0.32441 | 0.32096 | 0.31532
Notes: Test1.xlsx

## Slide 9: Test Result
· Order 2 (Normalize vs Non-Normalize)
Chart: Real Part of n2
10μm | 0.76499 | 0.76706 | 0.76545 | 0.76735 | 0.76962 | 0.77163 | 0.76969 | 0.77192 | 0.77392 | 0.77599 | 0.77409 | 0.77617 | 0.77806 | 0.77606 | 0.77816 | 0.78016 | 0.78222 | 0.77989 | 0.78173 | 0.78371 | 0.78178 | 0.78366 | 0.78567 | 0.78756 | 0.78531 | 0.78725 | 0.78904 | 0.79102 | 0.78861 | 0.79048 | 0.79231 | 0.79004 | 0.7918 | 0.7937 | 0.79539 | 0.79302 | 0.79467 | 0.7965 | 0.79815 | 0.79562 | 0.79716
15μm | 0.80172 | 0.80011 | 0.80243 | 0.80455 | 0.80287 | 0.80562 | 0.80805 | 0.80594 | 0.80839 | 0.80649 | 0.80846 | 0.81076 | 0.80872 | 0.81069 | 0.81301 | 0.81097 | 0.81312 | 0.81536 | 0.81321 | 0.81569 | 0.8178 | 0.81533 | 0.81764 | 0.81978 | 0.81687 | 0.81928 | 0.82076 | 0.81855 | 0.82102 | 0.82272 | 0.81993 | 0.82147 | 0.82394 | 0.82142 | 0.82292 | 0.82463 | 0.82261 | 0.824 | 0.82599 | 0.82738 | 0.82478
20μm | 0.81993 | 0.82288 | 0.82562 | 0.82292 | 0.8254 | 0.82323 | 0.82595 | 0.82791 | 0.82527 | 0.82795 | 0.82591 | 0.82833 | 0.82985 | 0.82747 | 0.82867 | 0.83094 | 0.82897 | 0.82944 | 0.83239 | 0.83287 | 0.83081 | 0.83377 | 0.83418 | 0.8321 | 0.83251 | 0.83293 | 0.83585 | 0.83877 | 0.83405 | 0.83698 | 0.83734 | 0.83513 | 0.84064 | 0.83838 | 0.83875 | 0.84164 | 0.83677 | 0.83966 | 0.83998 | 0.83765 | 0.83796
25μm | 0.83443 | 0.8324 | 0.83293 | 0.83595 | 0.83388 | 0.83689 | 0.83734 | 0.83522 | 0.83822 | 0.83864 | 0.84164 | 0.83684 | 0.83982 | 0.84021 | 0.83796 | 0.84094 | 0.84129 | 0.83897 | 0.8446 | 0.84227 | 0.84522 | 0.84554 | 0.84312 | 0.84071 | 0.84639 | 0.84397 | 0.84424 | 0.84174 | 0.84201 | 0.84495 | 0.8452 | 0.84266 | 0.84561 | 0.8458 | 0.84326 | 0.84899 | 0.84641 | 0.84661 | 0.84395 | 0.84694 | 0.84708
30μm | 0.8446 | 0.84232 | 0.83998 | 0.84301 | 0.84066 | 0.84639 | 0.84403 | 0.8416 | 0.84192 | 0.84492 | 0.84519 | 0.84271 | 0.8457 | 0.84316 | 0.84341 | 0.84641 | 0.84384 | 0.84403 | 0.84699 | 0.84722 | 0.84461 | 0.84758 | 0.84777 | 0.85071 | 0.84521 | 0.84819 | 0.84547 | 0.84558 | 0.84852 | 0.84576 | 0.84587 | 0.84877 | 0.84885 | 0.85184 | 0.85188 | 0.84901 | 0.84619 | 0.852 | 0.84621 | 0.84915 | 0.84619
Chart: Real Part of n2
10μm | 0.76593 | 0.76994 | 0.76885 | 0.76682 | 0.77067 | 0.77316 | 0.77232 | 0.77657 | 0.77753 | 0.76937 | 0.77698 | 0.77833 | 0.77903 | 0.78156 | 0.78216 | 0.78202 | 0.78324 | 0.78573 | 0.78424 | 0.78848 | 0.78582 | 0.78751 | 0.7875 | 0.78923 | 0.78905 | 0.7923 | 0.78996 | 0.79466 | 0.79517 | 0.79729 | 0.79322 | 0.79539 | 0.79633 | 0.79825 | 0.80014 | 0.79939
15μm | 0.80186 | 0.80235 | 0.80729 | 0.80575 | 0.80389 | 0.8063 | 0.8099 | 0.81149 | 0.81115 | 0.8093 | 0.81034 | 0.81168 | 0.81298 | 0.81371 | 0.81682 | 0.81448 | 0.81644 | 0.81602 | 0.81697 | 0.82079 | 0.8173 | 0.82052 | 0.82208 | 0.82282 | 0.82175 | 0.82226 | 0.82136 | 0.82473 | 0.82582 | 0.82661 | 0.82625 | 0.8273 | 0.82721 | 0.82912 | 0.8263 | 0.82517
20μm | 0.82567 | 0.82299 | 0.82389 | 0.82451 | 0.82673 | 0.82479 | 0.82965 | 0.82875 | 0.83119 | 0.82887 | 0.82715 | 0.82959 | 0.83235 | 0.8313 | 0.83182 | 0.83388 | 0.83276 | 0.83443 | 0.83494 | 0.83737 | 0.8343 | 0.8346 | 0.83443 | 0.83556 | 0.83766 | 0.83509 | 0.83856 | 0.83855 | 0.8381 | 0.83779 | 0.83654 | 0.84156 | 0.83812 | 0.8421 | 0.84325 | 0.83984
25μm | 0.83407 | 0.83905 | 0.84025 | 0.83431 | 0.83584 | 0.8356 | 0.83803 | 0.83989 | 0.84203 | 0.84001 | 0.83838 | 0.83856 | 0.83856 | 0.84385 | 0.84144 | 0.84028 | 0.84301 | 0.84435 | 0.84144 | 0.84378 | 0.84259 | 0.84244 | 0.84668 | 0.84679 | 0.8468 | 0.84681 | 0.8474 | 0.84697 | 0.84512 | 0.8498 | 0.84673 | 0.84616 | 0.84746 | 0.84929 | 0.8504 | 0.84775
30μm | 0.84569 | 0.84473 | 0.84429 | 0.84465 | 0.84481 | 0.84243 | 0.84357 | 0.84581 | 0.84645 | 0.84294 | 0.84615 | 0.84633 | 0.84707 | 0.84528 | 0.84904 | 0.84757 | 0.84471 | 0.85019 | 0.84912 | 0.85085 | 0.84648 | 0.84966 | 0.85159 | 0.85143 | 0.85222 | 0.85003 | 0.85076 | 0.8507 | 0.84767 | 0.85137 | 0.8477 | 0.85105 | 0.84747 | 0.85244 | 0.84931 | 0.84889
Normalized
Non-Normalized
Notes: Test1.xlsx

## Slide 10: Test Result
· Order 2 (Normalize vs Non-Normalize)
Normalized
Non-Normalized
Chart: Imaginary part of n2
10μm | 0.96508 | 0.96336 | 0.95706 | 0.95516 | 0.95375 | 0.95201 | 0.94544 | 0.94401 | 0.94232 | 0.94072 | 0.93434 | 0.93279 | 0.93101 | 0.92462 | 0.92314 | 0.92155 | 0.92004 | 0.91339 | 0.91166 | 0.91009 | 0.90402 | 0.90237 | 0.90089 | 0.89926 | 0.89295 | 0.89142 | 0.88972 | 0.88827 | 0.88189 | 0.88033 | 0.87872 | 0.87262 | 0.87097 | 0.86949 | 0.86778 | 0.86167 | 0.85994 | 0.85843 | 0.85673 | 0.85056 | 0.84877
15μm | 0.83664 | 0.82998 | 0.82743 | 0.82467 | 0.81808 | 0.81603 | 0.81366 | 0.80675 | 0.80446 | 0.79787 | 0.79514 | 0.79275 | 0.78615 | 0.78348 | 0.78117 | 0.7747 | 0.77225 | 0.76992 | 0.76347 | 0.76139 | 0.75897 | 0.75233 | 0.75015 | 0.74781 | 0.74089 | 0.73885 | 0.73596 | 0.7298 | 0.72784 | 0.72519 | 0.71864 | 0.7159 | 0.71398 | 0.70777 | 0.70505 | 0.70252 | 0.69684 | 0.69407 | 0.69183 | 0.68907 | 0.68304
20μm | 0.71864 | 0.71577 | 0.71274 | 0.70505 | 0.70184 | 0.69474 | 0.69179 | 0.68822 | 0.68087 | 0.67795 | 0.67121 | 0.66813 | 0.66432 | 0.65745 | 0.65346 | 0.65034 | 0.64393 | 0.63945 | 0.63692 | 0.63249 | 0.62619 | 0.62371 | 0.61932 | 0.61313 | 0.6088 | 0.60451 | 0.60206 | 0.59961 | 0.59172 | 0.58932 | 0.58509 | 0.57914 | 0.57852 | 0.57259 | 0.56847 | 0.5661 | 0.55851 | 0.55617 | 0.55211 | 0.54637 | 0.54235
25μm | 0.61715 | 0.60987 | 0.60451 | 0.60099 | 0.59385 | 0.59037 | 0.58509 | 0.5781 | 0.57467 | 0.56948 | 0.5661 | 0.55749 | 0.55413 | 0.54907 | 0.54235 | 0.53906 | 0.53407 | 0.52746 | 0.52584 | 0.5193 | 0.51606 | 0.5112 | 0.50476 | 0.49837 | 0.49678 | 0.49047 | 0.48575 | 0.4795 | 0.47486 | 0.47175 | 0.46713 | 0.46104 | 0.45797 | 0.45341 | 0.44744 | 0.44586 | 0.43994 | 0.43549 | 0.42963 | 0.42667 | 0.42226
30μm | 0.52584 | 0.51832 | 0.51085 | 0.50669 | 0.49933 | 0.49678 | 0.48953 | 0.48232 | 0.47672 | 0.47269 | 0.46713 | 0.46012 | 0.45615 | 0.44923 | 0.44384 | 0.43994 | 0.43317 | 0.42787 | 0.42401 | 0.41878 | 0.41222 | 0.40842 | 0.40329 | 0.39949 | 0.39178 | 0.38806 | 0.38177 | 0.37681 | 0.37314 | 0.36699 | 0.36213 | 0.3585 | 0.35368 | 0.35011 | 0.34534 | 0.33945 | 0.33365 | 0.33127 | 0.32441 | 0.32096 | 0.31532
Chart: Imaginary part of n2
10μm | 0.96399 | 0.9649 | 0.95899 | 0.95535 | 0.95207 | 0.95132 | 0.94647 | 0.94777 | 0.94461 | 0.93424 | 0.93509 | 0.93307 | 0.93023 | 0.92946 | 0.92605 | 0.91713 | 0.91504 | 0.91441 | 0.90907 | 0.91007 | 0.89849 | 0.89708 | 0.89368 | 0.89219 | 0.88827 | 0.88351 | 0.87767 | 0.87964 | 0.87684 | 0.87561 | 0.86293 | 0.8622 | 0.86012 | 0.85903 | 0.85767 | 0.84878
15μm | 0.83501 | 0.83079 | 0.83076 | 0.82333 | 0.81657 | 0.81461 | 0.81383 | 0.81094 | 0.80576 | 0.79823 | 0.79463 | 0.79174 | 0.78879 | 0.78523 | 0.78364 | 0.77123 | 0.76906 | 0.76464 | 0.76147 | 0.76069 | 0.74761 | 0.74672 | 0.74428 | 0.74107 | 0.736 | 0.72675 | 0.72227 | 0.72155 | 0.71877 | 0.71554 | 0.70574 | 0.70313 | 0.69954 | 0.69758 | 0.69151 | 0.68131
20μm | 0.72225 | 0.7148 | 0.71013 | 0.7037 | 0.70072 | 0.69427 | 0.69357 | 0.68798 | 0.68487 | 0.67614 | 0.67014 | 0.66755 | 0.66518 | 0.65974 | 0.65531 | 0.64572 | 0.64048 | 0.63738 | 0.63339 | 0.63065 | 0.61748 | 0.61354 | 0.60923 | 0.60588 | 0.60307 | 0.5906 | 0.58904 | 0.58505 | 0.58069 | 0.57634 | 0.56516 | 0.5647 | 0.55859 | 0.55738 | 0.55419 | 0.54182
25μm | 0.61582 | 0.61406 | 0.60922 | 0.59736 | 0.59329 | 0.588 | 0.5846 | 0.58076 | 0.57689 | 0.56811 | 0.5621 | 0.55735 | 0.55248 | 0.55106 | 0.54442 | 0.53168 | 0.52872 | 0.52489 | 0.51844 | 0.5151 | 0.50277 | 0.4982 | 0.49621 | 0.49182 | 0.48726 | 0.47591 | 0.47194 | 0.46744 | 0.46212 | 0.46031 | 0.44764 | 0.44323 | 0.43982 | 0.43666 | 0.43306 | 0.42101
30μm | 0.5257 | 0.51939 | 0.51324 | 0.50541 | 0.50004 | 0.49321 | 0.48849 | 0.48438 | 0.47922 | 0.46945 | 0.46604 | 0.46097 | 0.45621 | 0.45012 | 0.44687 | 0.43348 | 0.42708 | 0.42492 | 0.41949 | 0.41539 | 0.40114 | 0.39791 | 0.39409 | 0.38935 | 0.38499 | 0.37224 | 0.36807 | 0.3636 | 0.35783 | 0.35491 | 0.34209 | 0.33919 | 0.33355 | 0.33127 | 0.32583 | 0.3148
Notes: Test1.xlsx

## Slide 11: Test Result
· Order 3
Chart: Real Part of n2
10μm | -0.00025225 | -0.00022508 | -0.00023482 | -0.00024976 | -0.00023079 | -0.00019621 | -0.00018979 | -0.00021631 | -0.00020197 | -0.00016238 | -0.00017625 | -0.00019502 | -0.00017185 | -0.00013352 | -0.00017667 | -0.00017649 | -0.00012396 | -0.00015526 | -0.00016881 | -0.00012851 | -0.00014428 | -0.00017145 | -0.00012214 | -0.00014404 | -0.00015865 | -0.00011613 | -0.00015372 | -0.00015604 | -9.8969e-05 | -0.00017166 | -0.0001558 | -0.00013594 | -0.00017285 | -0.00012346 | -0.0001814 | -0.00017194 | -0.00014379 | -0.00020034 | -0.00015658 | -0.00020759 | -0.00020054
15μm | -0.00020287 | -0.00021505 | -0.00029148 | -0.00031204 | -0.00032326 | -0.00030261 | -0.00030393 | -0.0003883 | -0.00042071 | -0.00041903 | -0.0003638 | 0.00045684 | 0.00043047 | 0.00044121 | 0.00047217 | 0.00035359 | 0.00033851 | 0.00039175 | 0.00030268 | 0.00024405 | 0.000279 | 0.00023607 | 0.00014345 | 0.00015166 | 0.00013255 | 4.0057e-05 | 6.93e-05 | -1.0401e-05 | -8.2417e-05 | -5.2306e-05 | -0.00017688 | -0.00020001 | -0.00016953 | -0.00032985 | -0.00029257 | -0.00041805 | -0.00046052 | -0.00042921 | 0.0005492 | -0.00055329 | 0.00043208
20μm | -0.00017688 | -0.00024662 | -0.00031017 | -0.00029257 | -0.0003289 | -0.00049791 | 0.0005492 | 0.00049668 | 0.00053067 | 0.00035983 | 0.00024554 | 0.00020257 | 0.00023516 | 1.4401e-05 | -8.4168e-05 | -8.2493e-05 | -0.00023148 | -0.0003921 | -0.00041773 | -0.00053131 | 0.00058411 | 0.00062458 | 0.00044027 | 0.00027395 | 0.0002965 | 6.6566e-05 | -2.2461e-05 | -5.1135e-05 | -0.00032615 | -0.00031423 | -0.00056948 | -0.00068619 | 0.00070397 | 0.00044286 | 0.00055218 | 0.00020935 | 0.00018946 | -0.00011165 | -0.00016538 | -0.00037656 | -0.00054282
25μm | 0.00049359 | 0.00032149 | 6.6566e-05 | -0.00010718 | -0.00017109 | -0.00024615 | -0.00056948 | 0.00070931 | 0.00066057 | 0.00047302 | 0.00020935 | 0.00011632 | -5.8965e-06 | -0.00037683 | -0.00054282 | -0.00060266 | 0.00060677 | 0.00053972 | 0.00029103 | -2.1068e-05 | -3.8971e-05 | -0.00046334 | -0.00061247 | -0.00082965 | 0.0005573 | 0.00055713 | 5.0153e-05 | 6.4773e-05 | -0.00045761 | -0.00056508 | 0.00089047 | 0.0007122 | 0.00038463 | 0.00014868 | -0.00015867 | -0.0004264 | -0.00075512 | 0.00094227 | 0.00058216 | 0.00040075 | -6.2574e-05
30μm | 0.00029103 | -7.3513e-05 | -0.0002839 | -0.00034476 | 0.00085728 | 0.0005573 | 0.00049111 | 3.7061e-05 | -0.0003262 | -0.00038776 | 0.00089047 | 0.00058495 | 0.00047424 | -0.00017213 | -0.00035619 | -0.00075512 | 0.00083255 | 0.00064127 | 1.8158e-05 | 2.5728e-05 | -0.00074499 | -0.00084327 | 0.00056543 | 0.00040025 | -0.00022721 | -0.00051325 | -0.0010715 | 0.00096683 | 0.00023501 | 0.00016085 | -0.00068332 | -0.00076111 | 0.00065231 | 0.00048315 | -0.00016752 | -0.00067054 | -0.00098529 | 0.00068154 | 0.00054806 | -0.00030003 | -0.00077393
Chart: Imaginary part of n2
10μm | 0.0012551 | 0.0011147 | 0.0011579 | 0.0012259 | 0.0011279 | 0.0009543 | 0.00091908 | 0.0010426 | 0.00096881 | 0.00077542 | 0.00083761 | 0.00092239 | 0.00080919 | 0.00062562 | 0.0008238 | 0.00081926 | 0.00057255 | 0.00071361 | 0.00077211 | 0.00058509 | 0.00065362 | 0.00077287 | 0.00054783 | 0.00064281 | 0.00070449 | 0.00051323 | 0.00067598 | 0.00068272 | 0.0004308 | 0.00074345 | 0.00067133 | 0.00058275 | 0.00073747 | 0.00052401 | 0.00076603 | 0.00072234 | 0.00060092 | 0.00083296 | 0.00064762 | 0.00085417 | 0.00082086
15μm | 0.00080889 | 0.000851 | 0.001144 | 0.001215 | 0.0012487 | 0.0011595 | 0.0011553 | 0.0014643 | 0.0015738 | 0.0015549 | 0.0013391 | 0.001668 | 0.001559 | 0.001585 | 0.0016824 | 0.0012497 | 0.0011867 | 0.0013621 | 0.0010438 | 0.00083476 | 0.00094645 | 0.00079426 | 0.00047871 | 0.00050192 | 0.00043507 | 0.0001304 | 0.00022372 | 3.3301e-05 | 0.00026168 | 0.0001647 | 0.00055236 | 0.00061938 | 0.00052063 | 0.0010045 | 0.00088357 | 0.001252 | 0.0013681 | 0.0012644 | 0.0016044 | 0.0016027 | 0.0012412
20μm | 0.00055236 | 0.0007616 | 0.00094728 | 0.00088357 | 0.00098254 | 0.0014709 | 0.0016044 | 0.0014347 | 0.0015158 | 0.0010163 | 0.00068594 | 0.00055956 | 0.00064227 | 3.8903e-05 | 0.0002248 | 0.00021791 | 0.00060456 | 0.0010125 | 0.0010668 | 0.0013414 | 0.0014585 | 0.0015422 | 0.0010748 | 0.00066134 | 0.0007078 | 0.0001571 | 5.2415e-05 | 0.000118 | 0.00074422 | 0.00070897 | 0.0012702 | 0.0015133 | 0.001535 | 0.00095482 | 0.0011773 | 0.00044134 | 0.0003949 | 0.00023008 | 0.00033694 | 0.00075866 | 0.0010812
25μm | 0.0011983 | 0.00076944 | 0.0001571 | 0.00024942 | 0.00039253 | 0.00055683 | 0.0012702 | 0.0015602 | 0.0014324 | 0.0010112 | 0.00044134 | 0.00024173 | 1.2083e-05 | 0.00076125 | 0.0010812 | 0.0011835 | 0.0011748 | 0.0010302 | 0.00054754 | 3.9077e-05 | 7.1271e-05 | 0.00083531 | 0.0010884 | 0.0014532 | 0.00096242 | 0.00094824 | 8.4151e-05 | 0.00010711 | 0.0007459 | 0.00090786 | 0.0014101 | 0.0011112 | 0.00059146 | 0.0002253 | 0.00023699 | 0.00062755 | 0.001095 | 0.0013462 | 0.00081962 | 0.00055581 | 8.551e-05
30μm | 0.00054754 | 0.00013598 | 0.00051614 | 0.00061616 | 0.0015061 | 0.00096242 | 0.00083358 | 6.1827e-05 | 0.0005348 | 0.0006247 | 0.0014101 | 0.00091013 | 0.00072512 | 0.00025857 | 0.00052573 | 0.001095 | 0.0011861 | 0.00089739 | 2.4959e-05 | 3.474e-05 | 0.00098788 | 0.0010982 | 0.000723 | 0.00050252 | 0.00028009 | 0.0006211 | 0.0012727 | 0.0011273 | 0.0002689 | 0.00018057 | 0.00075271 | 0.00082248 | 0.00069131 | 0.00050215 | 0.00017072 | 0.00066995 | 0.00096488 | 0.00065405 | 0.00051542 | 0.00027639 | 0.00069837
Notes: Test1.xlsx

## Slide 12: Result
  Mis-understand with equation
  There might be some mistake during the simplification of the equation, especially for block2.
  Parameter Errors:

## Slide 13: Guesses
  Fatal error in Normalization
  There might be some mistake during the simplification of the equation, especially for block2.

## Slide 14: Possible Solutions
  Equation Deduce Error:
    Goes back to a further lower level of the equation and test again.
  Data Error:
    Use other data to test files instead. (planning to try it tonight)